# 09 9300 	VOLATILE ORGANIC COMPOUND (VOC) LIMITS FOR POLYURETHANES AND VARNISHES

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of reduced-emission polyurethanes and varnishes. Additional considerations related to product toxicity or other High Performance building criteria are included where appropriate.

PART 1 - GENERAL

1.01  SUMMARY

- This Section includes recommendations for volatile organic compound (VOC) content in polyurethanes and varnishes.

  - REFERENCES / QUALITY ASSURANCE

(for indoor air quality criteria)

- Polyurethanes and Varnishes:

South Coast Air Quality Management District Rule #1113 – Architectural Coatings, amended 5/14/99, South Coast Air Quality Management District (SCAQMD), State of California, www.aqmd.gov

1.04 SUBMISSION REQUIREMENTS

A	Manufacturer’s certification of product compliance with polyurethane and varnish requirements per section 2.01 of this specification.

- Material Safety Data Sheets.

- Manufacturer’s maintenance and cleaning instructions.

1.05	DELIVERY AND STORAGE

- To the extent feasible, do not store polyurethane or varnish products with materials that have a high capacity to adsorb VOC emissions (i.e., materials which are woven, fibrous or porous in nature, such as acoustical ceilings, carpet, textiles, etc.). Do not store polyurethane or varnish products in occupied spaces.

PART 2 – PRODUCTS

2.01 MATERIALS

- Environmentally-Preferable Product Criteria:

1.	Polyurethanes and Varnishes:

The volatile organic compound (VOC) content of polyurethane or varnish products shall not exceed 350 grams/liter, less water and less exempt compounds (as determined by U.S. EPA Reference Test Method 24).

PART 3 –  EXECUTION

3.01	INSTALLATION

- Comply, at minimum, with polyurethane or varnish manufacturer recommendations for space ventilation during and after installation. Where feasible, the following ventilation conditions shall be maintained during the polyurethane or varnish curing period, or for 72 hours after installation: 1) supply 100% outside air 24 hours a day; 2) supply airflow at a rate of 6 air changes per hour, when outside temperatures are between 55 degrees F and 85 degrees F and humidity is between 30% and 60%; and 3) supply airflow at a rate of 1.5 air changes per hour, when outside air conditions are not within the range stipulated in item 2 above.

- To the extent practical, allow polyurethane or varnish installations to cure prior to the installation of materials that adsorb VOCs. Materials that adsorb VOCs include carpets, textiles, unprimed gwb, and acoustical ceiling panels.

END OF SECTION 09932