# 09 9323.13	VOLATILE ORGANIC COMPOUND (VOC) LIMITS FOR WOOD STAINS

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of reduced-emission wood stain products. Additional considerations related to product toxicity or other High Performance building criteria are included where appropriate.

PART 1 – GENERAL

1.01  SUMMARY

- This Section includes recommendations for volatile organic compound (VOC) content in interior, field-applied wood stains.

  - REFERENCES / QUALITY ASSURANCE

(for indoor air quality criteria)

A.	South Coast Air Quality Management District Rule #1113, Architectural Coatings, amended May 14, 1999, South Coast Air Quality Management District (SCAQMD), State of California, www.aqmd.gov

1.03	RELATED DOCUMENTS

A	Environmentally-Preferable Products Specifications Section 09932 (Volatile Organic Compound (VOC) Limits For Polyurethanes And Varnishes), as included in the New York City Department of Design and Construction Design Guide for Consultants.

1.04 SUBMISSION REQUIREMENTS

A.	Manufacturer’s certification of product compliance with wood stain standards per section 2.01 of this specification.

- Material Safety Data Sheets.

1.05	DELIVERY AND STORAGE

- To the extent feasible, do not store wood stains with materials that have a high capacity to adsorb VOC emissions (i.e., materials which are woven, fibrous or porous in nature, such as acoustical ceilings, carpet, textiles, etc.). Do not store wood stains in occupied spaces.

PART 2 – PRODUCTS

2.01 MATERIALS

A.	Environmetally-Preferable Product Criteria:

1.	Wood Stains:

The volatile organic compound (VOC) content of wood stains shall not exceed 350 grams/liter, less water and less exempt compounds (as determined by U.S. EPA Reference Test Method 24).

PART 3 –  EXECUTION

3.01	INSTALLATION

- Comply, at minimum, with wood stain manufacturer recommendations for space ventilation during and after installation. Where feasible, the following ventilation conditions shall be maintained during the wood stain curing period, or for 72 hours after installation: 1) supply 100% outside air 24 hours a day; 2) supply airflow at a rate of 6 air changes per hour, when outside temperatures are between 55 degrees F and 85 degrees F and humidity is between 30% and 60%; and 3) supply airflow at a rate of 1.5 air changes per hour, when outside air conditions are not within the range stipulated in item 2 above.

- To the extent practical, allow wood stain installations to cure prior to the installation of materials that adsorb VOCs. Materials that adsorb VOCs include carpets, textiles, unprimed gwb, and acoustical ceiling panels.

END OF SECTION 09933