# PLASTIC& WOOD/PLASTIC

# 06 0000 	COMPOSITE LUMBER

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of post-consumer/post-industrial recycled content in plastic and wood/plastic composite lumber. Additional considerations related to product emissions, product toxicity, or other High Performance building criteria are included where appropriate.

PART 1 - GENERAL

1.01  SUMMARY

- This section includes plastic and wood/plastic composite lumber which meets specified criteria for:

- Post-consumer and/or post-industrial recycled content in plastic lumber.

- Post-consumer and/or post-industrial recycled content in composite wood/plastic lumber.

- Applicable products made partially or entirely from plastic and wood/plastic composite lumber include, but are not limited to, the following:

- Dimensional lumber, Landscape Timbers, and Decking

- Traffic Control Items (e.g., Parking Stops, Speed Bumps)

- Site Furnishings (benches, tables, waste receptacles)

- Playground Structures

- Fencing

- Signage

  - REFERENCES / QUALITY ASSURANCE

(for recycled content and other High Performance building criteria)

- Recycled content:

- EPA Comprehensive Procurement Guidelines, www.epa.gov/cpg

- Performance criteria (include applicable criteria depending on the product type):

- ASTM D6341-98 Standard Test Method for Determination of the Linear Coefficient of Thermal Expansion of Plastic Lumber and Plastic Lumber Shapes Between -30 and 140°F (-34.4 and 60°C)

- ASTM D6435-99 Standard Test Method for Shear Properties of Plastic Lumber and Plastic Lumber Shapes

ASTM D6111-97 Standard Test Method for Bulk Density and Specific Gravity of Plastic Lumber and Shapes by Displacement

- ASTM D6108-97 Standard Test Method for Compressive Properties of Plastic Lumber and Shapes

- ASTM D6117-97 Standard Test Methods for Mechanical Fasteners In Plastic Lumber and Shapes

- ASTM D6112-97 Standard Test Methods for Compressive and Flexural creep and Creep-Rupture of Plastic Lumber and Shapes

- ASTM D6109-97 Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastic Lumber

1.03	SUBMISSION REQUIREMENTS

A	Manufacturer’s certification of recycled content per section 2.01 of this specification.

- Material Safety Data Sheets.

- Manufacturer’s maintenance and cleaning instructions.

- Manufacturer’s policy statement on plastic & wood/plastic composite lumber recycling programs.

PART 2 – PRODUCTS

2.01 MATERIALS

- Environmental Criteria:

- Recycled Content:

Plastic and wood/plastic composite lumber shall contain recycled content material as follows:

- Plastic Lumber, including High Density Polyurethane (HDPE), HDPE/Fiberglass composites, and Mixed Resin Composites: a minimum of 75% (combined) post-industrial/post-consumer recycled content with a minimum of 50% post-consumer recycled content.

- Composite Wood Fiber and Plastic Lumber: a minimum of 100% (combined) post-industrial/post-consumer recycled content, with a minimum of 50% post-consumer recycled content.

The percentage of recycled content is based on the weight of the component materials.

PART 3 –  EXECUTION

3.01	INSTALLATION

- Follow manufacturer’s recommendations for material installation, including requirements for structural support, thermal movement, working, fastening, and finishing (where applicable).

3.02	WASTE MANAGEMENT

- Identify manufacturer’s policy for collection or return of construction scrap, unused material, demolition scrap, and/or packaging material. Where feasible, institute demolition and construction waste separation and recycling to take advantage of manufacturer’s programs.

END OF SECTION 06512