# 09 2900 	GYPSUM WALLBOARD

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of post-consumer/post-industrial recycled content in gypsum wallboard. Additional considerations related to product emissions, product toxicity, or other High Performance building criteria are included where appropriate.

PART 1 - GENERAL

1.01  SUMMARY

- This section includes gypsum wallboard assemblies which meet specified criteria for:

- Post-consumer recycled paper content in the gypsum wallboard paper facing; and

- Post-industrial recycled content (synthetic gypsum) in the gypsum wallboard cores (optional).

1.02	SUBMISSION REQUIREMENTS

A	Manufacturer’s certification of recycled content per section 2.01 of this specification.

- Material Safety Data Sheets.

- Manufacturer’s maintenance instructions.

- Manufacturer’s policy statement on gypsum wallboard recycling programs.

1.03	DELIVERY AND STORAGE

- Gypsum wallboard to be stored per manufacturer’s recommendations for allowable temperature and humidity range. Panels shall not be allowed to become damp.

- Where feasible, gypsum wallboard shall not be stored with materials which have high emissions of VOCs or other contaminants (see section 3.01 below).

PART 2 – PRODUCTS

2.01 MATERIALS

- Environmental Criteria:

- Recycled Content:

Gypsum wallboard shall contain recycled content material as follows:

- Paper facings: a minimum of 100% post-consumer recycled paper content.

- Gypsum cores: Where feasible, a minimum of 75% post-industrial recycled gypsum content (also called “synthetic” gypsum – from coal-fired power plants).

The percentage of recycled content is based on the weight of the component materials.

PART 3 –  EXECUTION

3.01	INSTALLATION

- Where feasible, one or both of the following procedures shall be used to minimize the exposure of gypsum wallboard to materials or finishes which have high short-term emissions of VOC’s, formaldehyde, particulates, or other air-borne compounds:

- The gypsum wall board shall be taped, spackled and primed before the installation of the highly-emitting materials.

- The gypsum wallboard shall be installed after the installation of the highly-emitting materials.

Materials with high short-term emissions include, but are not limited to: adhesives, sealants and glazing compounds (specifically those with petrochemical vehicles or carriers); paint, wood preservatives, and finishes; control and/or expansion joint fillers; hard finishes requiring adhesive installation; gypsum board (with associated finish processes and products); and composite or engineered wood products with formaldehyde binders.

3.02	WASTE MANAGEMENT

- Identify manufacturer’s policy for collection or return of construction scrap, unused material, demolition scrap, and/or packaging material. Where feasible, institute demolition and construction waste separation and recycling to take advantage of manufacturer’s programs.

END OF SECTION 09250