# 32 1800 	ATHLETIC & RECREATIONAL SURFACES

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of post-consumer/post-industrial recycled content in athletic & recreational surfaces. Additional considerations related to product emissions, product toxicity, or other High Performance building criteria are included where appropriate.

PART 1 - GENERAL

1.01  SUMMARY

- This section includes athletic & recreational surfaces which meet specified criteria for post-consumer and/or post-industrial recycled content.

  - REFERENCES / QUALITY ASSURANCE

(for recycled content and other High Performance building criteria)

- Recycled content:

- EPA Comprehensive Procurement Guidelines, www.epa.gov/cpg

1.03	SUBMISSION REQUIREMENTS

A	Manufacturer’s certification of recycled content per section 2.01 of this specification.

- Material Safety Data Sheets.

- Manufacturer’s maintenance and cleaning instructions.

- Manufacturer’s policy statement on athletic & recreational surfaces recycling programs.

1.04	DELIVERY AND STORAGE

- Where feasible, do not store rubber athletic & recreational surface products with materials that have a high capacity to adsorb VOC emissions (i.e., materials which are woven, fibrous or porous in nature, such as acoustical ceilings, carpet, textiles, etc.). Do not store exposed rubber athletic & recreational surface materials in occupied spaces.

PART 2 – PRODUCTS

2.01 MATERIALS

- Environmental Criteria:

- Recycled Content:

Athletic & recreational surfaces shall contain recycled content material as follows (depending upon the constituent materials used):

- Rubber: a minimum of 70% (combined) post-industrial/post-consumer recycled tire rubber content.

- Plastic: a minimum of 25% (combined) post-industrial/post-consumer recycled content.

- Composite plastic & rubber: a minimum of 70% (combined) post-industrial/post-consumer recycled tire rubber and plastic content.

The percentage of recycled content is based on the dry weight of the raw materials, exclusive of any additives such as adhesives, binders, or coloring agents.

PART 3 –  EXECUTION

3.01	WASTE MANAGEMENT

- Identify athletic & recreational surface manufacturer’s policy for collection or return of construction scrap, unused material, demolition scrap, and/or packaging material. Where feasible, institute demolition and construction waste separation and recycling to take advantage of manufacturer’s programs.

END OF SECTION 02790